## Slide 1: Fate and Behaviour of Vanadium During the Aerobic Neutralisation of Alkaline Steel Slag Leachate
Andrew. J. Hobson1, Douglas. I. Stewart2, Andrew W. Bray1, William M. Mayes3, Alex L. Riley3 and Ian T. Burke1
1School of Earth and Environment and 2School of Civil Engineering, University of Leeds.
3Centre for Environmental and Marine Sciences, University of Hull

## Slide 2: Leachate generation
Rainwater
Steel Slags

## Slide 3: Ca(OH)2 / β-Ca2SiO4 dissolution
Rainwater
Steel Slags
Alkalinity generation & V-release
CaO + H2O → Ca2+ + 2OH-
β-Ca2Si(V)O4 (s) + 2H2O → 2Ca2+ + H2SiO42- + 2OH- + VO43-
Secondary V-containing phases
3Ca2+ + 2H2SiO42- + OH- (+ xVO43-) → 3CaO·2SiO2(xVO4)·3H2O (s)
3Ca2+ + 2VO43- ⇌ Ca3(VO4)2 (s)

## Slide 4: Ca3(VO4)2 Solubility
Log Ksp = -17.97
Hobson et al., in prep
[V] concentrations limited by [Ca] controlling secondary phase
8 pH 12.5

## Slide 5: Leachate springs
Groundwater outflow
Steel Slags
CO2 in gassing
River flow→

## Slide 6: CaCO3 precipitation
Groundwater outflow
Steel Slags
CO2 in gassing
CO2 In gassing
CO2 (g) ⇌ CO2 (aq) CO2 + H2O ⇌ H2CO3 H2CO3 ⇌ HCO3- + H+ ⇌ CO32- + H+ H+ + OH- ⇌ H2O Ca2+ + CO32- ⇌ CaCO3 (s)
Overall reaction
Ca2+ + CO2 + 2OH- → CaCO3 (s) + H2O

## Slide 7
Consett Steel Works, Co. Durham, UK

## Slide 8: Site Data – Howden Burn, Consett
Chart: Distance from dischanrge piont (m)
| 0 | 20 | 50 | 123 | 153 | 261 | 434.3 | 0 | 15 | 20 | 60 | 90 | 220 | 250 | 280 | 290 | 460 | 0 | 66.599999999999994 | 87.5 | 177.1 | 291.7 | 455.9 | 0 | 2 | 26 | 93 | 298
C/Co [K] | 1 | 1.0218 | 1.022 | 1.0165 | 1.0156 | 0.99111 | 1.0078 | 0.98113 | 1.0001 | 0.93646 | 1 | 0.88321 | 0.80985 | 0.91209 | 0.90432 | 0.9001 | 1 | 0.95263 | 0.95269 | 0.96344 | 1.0818
 | 1 | 0.83794 | 0.7467 | 0.2545 | 0.34214 | 0.39069 | 0 | 1 | 0.77351 | 0.67393 | 0.49284 | 0.33833 | 0.25234 | 0.038749 | 0 | 0 | 0 | 1 | 0.88598 | 0.56682 | 0.47314 | 0.2433
Chart: A) pH
| 0 | 20 | 50 | 123 | 153 | 261 | 434.3 | 0 | 15 | 20 | 60 | 90 | 220 | 250 | 280 | 290 | 460 | 0 | 66.599999999999994 | 87.5 | 177.1 | 291.7 | 455.9 | 0 | 2 | 26 | 93 | 298
pH | 11.6 | 11.4 | 11.3 | 11.2 | 11.2 | 10.4 | 9.9 | 12.68 | 12.45 | 12.48 | 12.39 | 12.36 | 12.34 | 12.56 | 12.15 | 12.33 | 11.95 | 11.51 | 11.56 | 11.56 | 11.56 | 11.4 | 11.32 | 11.73 | 11.66 | 11.63 | 11.49 | 10.88
Chart: B) Ca
| 0 | 20 | 50 | 123 | 153 | 261 | 434.3 | 0 | 15 | 20 | 60 | 90 | 220 | 250 | 280 | 290 | 460 | 0 | 66.599999999999994 | 87.5 | 177.1 | 291.7 | 455.9 | 0 | 2 | 26 | 93 | 298
C/Co [Ca] | 1 | 0.98403 | 0.95806 | 0.90776 | 0.87236 | 0.85364 | 0.82656 | 1 | 0.94647 | 0.94119 | 0.90834 | 0.88958 | 0.84934 | 0.83251 | 0.80272 | 0.76069 | 0.75594 | 1 | 0.9695 | 0.87831 | 0.86441 | 0.77517 | 0.6832 | 1 | 0.94656 | 0.88688 | 0.89324 | 0.81545
Chart: D) V
| 0 | 20 | 50 | 123 | 153 | 261 | 434.3 | 0 | 15 | 20 | 60 | 90 | 220 | 250 | 280 | 290 | 460 | 0 | 66.599999999999994 | 87.5 | 177.1 | 291.7 | 455.9 | 0 | 2 | 26 | 93 | 298
C/Co [V] | 1 | 0.9555 | 0.89431 | 0.81824 | 0.75954 | 0.67302 | 0.55462 | 1 | 0.92677 | 0.92152 | 0.90217 | 0.8388 | 0.81894 | 0.76642 | 0.74599 | 0.67063 | 0.61559 | 1 | 0.86471 | 0.84155 | 0.71762 | 0.66854 | 0.66746 | 1 | 0.89106 | 0.88363 | 0.89067 | 0.78246
Chart: E) Fe
| 0 | 20 | 50 | 123 | 153 | 261 | 434.3 | 0 | 15 | 20 | 60 | 90 | 220 | 250 | 280 | 290 | 460 | 0 | 66.599999999999994 | 87.5 | 177.1 | 291.7 | 455.9 | 0 | 2 | 26 | 93 | 298
C/Co [Fe] | 0.99993 | 0.89668 | 0.86022 | 0.86349 | 0.83532 | 0.69713 | 0.48365 | 0.99997 | 0.83247 | 0.78867 | 0.661 | 0.57816 | 0.56976 | 0.63883 | 0.49241 | 0.48368 | 0.46125 | 1 | 0.92514 | 0.82575 | 0.79176 | 0.72143
Co = 104 ±31 ppm
Co = 127 ±57 ppm
Co = 58 ±8 ppb
Si Co = 1300 ±340 ppb
Al Co = 129 ±39 ppb
Chart: C) K
| 0 | 20 | 50 | 123 | 153 | 261 | 434.3 | 0 | 15 | 20 | 60 | 90 | 220 | 250 | 280 | 290 | 460 | 0 | 66.599999999999994 | 87.5 | 177.1 | 291.7 | 455.9 | 0 | 2 | 26 | 93 | 298
C/Co [K] | 1 | 1.0551 | 1.06 | 1.0592 | 1.0445 | 0.97577 | 1.0145 | 1 | 0.9928 | 1.0043 | 0.99817 | 0.99567 | 0.99704 | 0.98706 | 0.98644 | 0.92215 | 0.91755 | 1 | 1.0701 | 1.021 | 1.0371 | 0.94072 | 0.93813 | 1 | 0.96293 | 0.94806 | 0.94725 | 0.97509
pH reduction & Ca removal
Concurrent Trace Metal Removal
No change in conservative elements (i.e. no dilution)

## Slide 9: Experimental
Slag Leachate
Site Leachate – Ca(OH)2 type ~35 ppb V (+Fe)
Slag Leachate – Ca2SiO4 type ~ 500 ppb V (+Si)
Sim. Leachate – 10 % Ca(OH)2 + 2500 ppb VO43- (for XAS)
All initially pH ~12 & CO2 free

## Slide 10: Results – pH

## Slide 11: Results – Calcium
Graph of C/Co [Ca] vs pH– three leachates CaCO3 only systems
Site [Ca] = 194 ppm
Slag [Ca] = 89 ppm
Sim. [Ca] = 75 ppm
Total [Ca] removal very similar in all systems; ~60-80 ppm

## Slide 12: Results – Vanadium
Graph of C/Co [V] vs pH– three leachates CaCO3 only systems
Site [V] = 35 ppb
Slag [V] = 510 ppb
Sim. [V] = 2510 ppb
[V] removed: Site = ~13 ppb; Slag = ~30 ppb; Sim. = 400 ppb

## Slide 13: Results – Fe
Site [Fe] = 166 ppb
Slag & Sim. [Fe] = n.d.
Sim. [Si] = n.d.
Site [Si] = 1.6 ppm
Slag [Si] = 21 ppm
Results – Si
60-70 ppb Fe removed in Site leachate system

## Slide 14: TEM – site leachate ppt
SAED
Calcite
Fe-O rich particles
Low res Bright field TEM
Hi res TEM
0.145 nm
0.250 nm
Chart: Energy (keV)
EDS spectra
Fe
Fe
Fe
Si
Ca
Ca
O
Cu
Na
C
P
S
Cl
Al

## Slide 15: Goethite amended systems
Graph of C/Co [V] vs pH– three leachates FeOOH systems
unamended data
Site
Slag
Sim.

## Slide 16: Vanadium K-edge XANES
Chart: Energy (eV)
0.5
V5+ aqueous
V5+-Kaolinite
V5+-Al(OH)3
V5+-FeOOH
Sim. +FeOOH
Slag +FeOOH
Site +FeOOH
Sim. +Kaolinite
Slag +Kaolinite
Site +Kaolinite
Sim. unamend
Slag unamend
Site unamend
Diamond Light Source, UK, Beamline i18
Data collected from CaCO3 precipitates (pH ~8)
All Vanadium present as V5+

## Slide 17: V – XANES interpretation
(Td) V5+
(Py) V5+
(Oh) V3+
(Oh) V5+
(Oh) V4+
(Py) V4+
V5+-Al(OH)3
V5+-FeOOH
NaVO3
Experimental Samples
Measurement uncertainty
V5+-Kaol.
Distortion in VO4 tetrahedral leads to reduced peak intensity
adsorption / incorporation

## Slide 18: V-FeOOH EXAFS
Chart: r (Å)
Peacock and Sherman, 2004
Chart: k (Å-1)
A)
B)
A) Sim. +FeOOH (0.2% w/w)
B) V-FeOOH std. (2% w/w)
VO4
V-Fe

## Slide 19: Conclusions
Groundwater outflow
Steel Slags
CO2 in gassing = modest V removal via sorption to neoformed phases
Interaction with stream sediments = complete V removal via adsorption to iron(oxy)hydroxides
Vanadium will accumulate in near field sediments; no far field impacts

## Slide 21
Chart: [Ca2+] mol L-1
| 0.1 | 0.01 | 1E-3 | 1E-4 | 1.0000000000000001E-5 | 9.9999999999999995E-7
[VO43-] | 3.2734e-08 | 1.0351e-06 | 3.2734e-05 | 0.0010351 | 0.032734 | 1.0351
 | 1.6845e-05
 | 9.6629e-06
 | 0.0005865
 | 1.6845e-05
 | 1.6845e-05
 | 1.6845e-05
 | 0.0005865
 | 1.6845e-05
 | 0.023
 | 2.9676e-07
 | 0.023
Oversaturated
Undersaturated
Calcite / atm. CO2
~4000 ppb V
Ca(OH)2
~15 ppb V
Aerobic expt. 1000-3000 ppb V
Ca2SiO4 / Ca-Si-H
Anaerobic expt.
200-500 ppb V
Site Leachates
20-100 ppb V
Acute Tox.
Chronic Tox.
280 ppb
19 ppb