## Slide 1
Establishment of a soil layer within bauxite residues using organic matter and gypsum
Andy Bray, Doug Stewart, Ronan Courtney, Will Mayes & Ian Burke

## Slide 2
Bauxite Residue/Red Mud
By product in the production of alumina (Al2O3)
1 ton Alumina = 1-2 tons of Red Mud
Since 2012 global annual alumina production > 100 million tonnes/year

## Slide 3
Lanjigarh, India
Stade, Germany
Hayes, Jamaica
Worsley, Australia
Barcarena, Brazil

## Slide 4
Red mud characteristics
~30 % wt. solids
Of those solids:
~30 % Fe oxides and (oxy)hydroxides
~10 % Al (oxy)hydroxides
NaOH
Ca(OH)2
Sodalite
Cancrinite
Sodalite Na6(Al6Si6O24).2NaOH
Cancrinite Na6(Al6Si6O24 ).2CaCO3
High pH
High salinity

## Slide 5
High alkalinity
High salinity
Mobility of potentially toxic metals (Al, V)

## Slide 6
Associated Press

## Slide 7
Palíndromo Mészaros

## Slide 8
Process sand
Organic matter
Gypsum
20 cm
20 cm
Process sand
Organic matter
Amended
No gypsum
Unamended

## Slide 9
20 years later…

## Slide 10
Unamended

## Slide 11
Unamended

## Slide 12
No gypsum

## Slide 13
Amended
Holcus lanatus – Yorkshire Fog
Trifolium pratense – Red Clover

## Slide 14
Amended
No gypsum
Unamended
Cancrinite/sodalite
Cancrinite

## Slide 15
AND GEOCHEMICAL DATA

## Slide 16
Amended
No gypsum
Unamended
Cancrinite/sodalite
Cancrinite

## Slide 17
Na
Al
V
H2O extraction Amended No gypsum Unamended

## Slide 18
Al
V
Al
V
High pH PO4 extraction Amended No gypsum Unamended

## Slide 19
Amended
Unamended

## Slide 20
Rhizobia
Rhizosphere fungi & bacteria
Plant symbiosis
Organic exudates
Amended
Unamended
pH buffering by organic acids?
~5 nanomoles litre-1

## Slide 21
NaOH
Ca(OH)2
Bauxite
Gibbsite, Boehmite, Diaspore
Goethite,
Haematite
Al oxyhydroxides
Fe oxyhydroxides
Titanium oxides
Al
Fe
Si, Ti
V(IV)
V(V)
High pH
High temp
Oxygen present
V(V)
Clays,
Anatase, Ilmenite
Bayer Process Characteristic Solids
(Cancrinite, Sodalite, Hydrogarnet)

## Slide 22
Sodalite
Cancrinite
Katoite
(Declercq, personal comms.)
Chart: pH
LOD | -6.2093 | -6.2093
(Burke et al., 2012)
Cancrinite

## Slide 23
Chart: pH
Al(OH)3 (am) | -8 | 0
Gibbsite | -10.8 | -2.8
LOD | -5.4681 | -5.4681
Chart: pH
LOD | -6.2093 | -6.2093
Al
V
Neutralisation:
Decreases feldspathoid dissolution – preventing Na and V release.
Reduces Al solubility

## Slide 24
High alkalinity
High salinity
Mobility of potentially toxic metals (Al, V)

## Slide 25
Process sand
Organic matter
Gypsum
20 cm
20 cm
20 Year
7 Year
Unamended
Process sand
Organic matter
Gypsum

## Slide 26
Na

## Slide 27
Al
V
H2O extraction

## Slide 28
Process sand
Improves substrate structure, stability, and drainage

## Slide 29
Process sand
Gypsum
1% w/w gypsum can buffer bauxite residue to pH 7.5-8.5.
Additional Ca binds to abundant OH
Improves substrate structure, stability, and drainage

## Slide 30
Process sand
Organic matter
Gypsum
1% w/w gypsum can buffer bauxite residue to pH 7.5-8.5.
Additional Ca binds to abundant OH
Improves substrate structure, stability, and drainage
Provides organic bound and available nutrients.
Friendlier environment for plant and rhizospheric life.

## Slide 31
Feldspathoid + Water ↔ Alkalinity + Salinity + stuffs
Surface organic activity increases CO2 penetration and produces H+
Shift to an organic controlled dynamic remediation means longer term stability

## Slide 32
Cap and cover estimate for 1.7km2 = €15 million
gypsum and organic matter estimate = €1.5 million
NERC R3AW grant: NE/L014211/1
Red Mud + gypsum + organic matter + sand =
↓ alkalinity
↓ salinity
↓ mobility