## Slide 1: µXANES investigation of the environmental behaviour of vanadium in BOF steel slag leachates
Andrew. J. Hobson1, Douglas. I. Stewart2, Andrew W. Bray1, William M. Mayes3, Michael Rogerson3, Alex L. Riley3 and Ian T. Burke1
1School of Earth and Environment and 2School of Civil Engineering, University of Leeds.
3Geography and Environmental Sciences, University of Hull

## Slide 2: Background: Steel slags
What? Primary byproduct of steel manufacture
How much? 2015: 170 - 250 million tonnes worldwide (USGS, 2015)
Use?
  Aggregate (civil engineering)
  Acid neutralisation (soils)
  CO2 sequestration
Problems?
Notes: Talk about recycling here too
High lime process – discuss CaO – Ca(OH)2 – CaCO3 issues

## Slide 3: Environmental impacts
Rainwater
Steel Slags
1. High pH leachate
CaO + H2O → Ca(OH)2
Ca(OH)2 → Ca2+ + 2OH-
Ca2SiO4 + 4H2O → 2Ca2+ + H4SiO4 + 4OH-
= pH 11.5 – 12.5

## Slide 4: Environmental impacts
Rainwater
Steel Slags
2. Rapid calcite deposition
Ca2+ + CO2 → CaCO3 (s) + H2O

## Slide 5: Environmental impacts
Rainwater
Steel Slags
3. Mobilisation of trace metals
e.g. V, Cr, Pb, Ni

## Slide 6: Vanadium in Steel Slags
Concentrated in steel slags from primary ores
430 – 1700 mg/kg in BOF slag (Proctor et al, 2000)
  This study ~700 mg/kg
Solubility/toxicity strongly influenced by oxidation state
Oxidation of V(IV) to V(V) implicated as mechanism leading to enhanced V leaching under aerobic conditions (Chaurand et al, 2007)
Notes: Despite toxicity of V (esp V(V)) little data re. leaching behaviour

## Slide 7: Part 1: Objectives & methods
Establish variation in V speciation before and after leaching under aerobic and anaerobic conditions
Samples leached for 6 months in Milli-Q water
SEM/EDS
  Characterise steel slag
    ID principal phases
    Locate V-bearing phases
XAS (XANES)
  Determine V speciation in:
    Unweathered material
    Aerobically weathered material
    Anaerobically weathered material
Notes: 3 aims – determine the principal mineral phases present in steel slag and which contained vanadium
Determine V speciation in unweathered material and weathered regions from both systems; aerobic and anaerobic – is there any variation between them? Do they offer any insights into mechanism of vanadium leaching from slags?
Used a variety of spectroscopy techniques including SEM imaging, EDS spot analysis and mapping and synchrotron data.

## Slide 8: Results: Vanadium release
Threshold values from http://response.restoration.noaa.gov/sites/default/files/SQuiRTs.pdf
Notes: Next was to work out where it was coming from!

## Slide 9: Slag composition
Ca-silicates
(Ca2SiO4)
CaO (free lime)
Brownmillerite
(dicalcium ferrite)
Wustite (FeO)
Notes: 4 phases – dominant dark purple phase is dicalcium silicate (aka larnite)
Purple phase is calcium oxide (aka free lime)
Light purple phase is dicalcium ferrite (aka brownmillerite)
Green phase is iron oxide (aka wustite)

## Slide 10: EDS
V
V
Ti
V is located in Ca-silicates and brownmillerite phases
(wt% 0.3 - 0.5% and 1.0 - 1.3% respectively)
Notes: Used EDS spot analysis on each phase to locate vanadium host phases and approximate abundance in each phase

## Slide 11: Leaching effects
Aerobic
Anaerobic
20-50 µm weathered ‘rind’ post-leaching
Notes: Leached ‘rind’ depleted in Ca/Si i.e. leaching of free lime and Ca-silicates has taken place.
Brownmillerite and wustite phases largely unaltered.
CSH formed in black regions – present throughout the rind.

## Slide 12: Calcium-Silicate-Hydrate formation
C-S-H
Ca2SiO4

## Slide 13: XANES analysis
Vanadate
V2O5 (V5+)
V2O5 (V4+)
Calcium silicate
Calcium silicate hydrate
Brownmillerite
Standards
Experimental samples
Notes: Spectra of experimental samples are similar to those of V(IV) and (V) standards

## Slide 14: V speciation
Chart: 
| 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1
Core | 5481.77 | 5480.96 | 5481.86 | 5480.11 | 5481.32 | 5480.76 | 5479.44 | 5479.23 | 5480.58 | 5481.55 | 5481.91 | 5482.09 | 5482.18 | 5482.09 | 5482.18 | 5481.59 | 5479.62 | 5482.4 | 5482.27 | 5481.55 | 5479.23 | 5481.28 | 5478.95 | 5478.91 | 5481.77 | 5480.29 | 5481.16 | 5481.41 | 5481.86 | 5482.09 | 5482 | 5480.56 | 5481.41 | 5481.73
Aerobic weathered | 5482.15 | 5479.57 | 5481.55 | 5482.18 | 5480.2 | 5479.87 | 5480.14 | 5481.97
Anaerobic weathered | 5481.37 | 5480.22 | 5481.03 | 5480.11 | 5479.64 | 5479.93 | 5481.44 | 5481.68 | 5481.21 | 5480.92
 | 5480.3 | 5480.3
 | 5479 | 5479
 | 5478 | 5478
Chart: 
| 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1
 | 0.90479 | 0.75049 | 0.48586 | 0.93192 | 0.43442 | 0.94283 | 0.81029 | 0.2242 | 0.7073 | 0.94635 | 0.91801 | 0.91014 | 0.9558 | 0.97784 | 0.93375 | 0.85188 | 0.95528 | 0.91643 | 0.96997 | 0.83141 | 0.28298 | 0.7889 | 0.36119 | 0.17225 | 0.96682 | 0.5677 | 0.92903 | 0.8755 | 0.8692 | 0.99988 | 0.92244 | 0.57504 | 0.76056 | 0.9432
 | 1.0093 | 0.60154 | 0.8755 | 0.93218 | 0.68971 | 0.2591 | 0.2095 | 0.93533
 | 0.87865 | 0.66924 | 0.80937 | 0.61413 | 0.50864 | 0.5147 | 0.8503 | 0.9495 | 0.84086 | 0.75111
 | 0.7 | 0.7
 | 0.4 | 0.4
E1/2
Pre-edge peak
V
V
IV/V
IV
IV
III/IV
III
Normalised pre-edge peak intensity
E1/2
Core
Aerobic rind
Anaerobic rind
Ca2SiO4
Brownmillarite
C-S-H

## Slide 15: Vanadium release and mobility
Rainwater
Steel Slags
V-release
β-Ca2Si(V)O4 (s) + 2H2O → 2Ca2+ + H2SiO42- + 2OH- + VO43-
Secondary V-containing phases
3Ca2+ + 2H2SiO42- + OH- (+ xVO43-) → 3CaO·2SiO2(xVO4)·3H2O (s)
3Ca2+ + 2VO43- ⇌ Ca3(VO4)2 (s)

## Slide 16: Ca3(VO4)2 Solubility
Log Ksp = -17.97
[V] concentrations limited by [Ca] controlling secondary phase
8 pH 12.5

## Slide 17: Part 1 Summary
V is located within Ca-silicates (0.3-0.5 wt%) as V(V) and brownmillerite (1.0-1.3 wt%) as V(IV/V)
V(V) released during dissolution of Ca-silicates:
  Ca2Si(V)O4(s) + 2H2O → 2Ca2+ + H2SiO42- + 2OH- + VO43-
Some V(V) incorporated into CSH (secondary phase):
3Ca2+ + 2H2SiO42- + OH- (+ xVO43-) → 3CaO·2SiO2·(xVO4)·3H2O (s)
High release in aerobic systems due to Ca sink to CaCO3 which allows continued dissolution of Ca-silicates and associated release of V
Formation of CSH has an armouring effect – crush and weather slag prior to use to reduce V release

## Slide 18: Part2: V mobility at Leachates springs
Groundwater outflow
Steel Slags
CO2 in gassing
River flow→

## Slide 19: CaCO3 precipitation
Groundwater outflow
Steel Slags
CO2 in gassing
CO2 In gassing
CO2 (g) ⇌ CO2 (aq) CO2 + H2O ⇌ H2CO3 H2CO3 ⇌ HCO3- + H+ ⇌ CO32- + H+ H+ + OH- ⇌ H2O Ca2+ + CO32- ⇌ CaCO3 (s)
Overall reaction
Ca2+ + CO2 + 2OH- → CaCO3 (s) + H2O

## Slide 20
Consett Steel Works, Co. Durham, UK

## Slide 21: Site Data – Howden Burn, Consett
Chart: Distance from dischanrge piont (m)
| 0 | 20 | 50 | 123 | 153 | 261 | 434.3 | 0 | 15 | 20 | 60 | 90 | 220 | 250 | 280 | 290 | 460 | 0 | 66.599999999999994 | 87.5 | 177.1 | 291.7 | 455.9 | 0 | 2 | 26 | 93 | 298
C/Co [K] | 1 | 1.0218 | 1.022 | 1.0165 | 1.0156 | 0.99111 | 1.0078 | 0.98113 | 1.0001 | 0.93646 | 1 | 0.88321 | 0.80985 | 0.91209 | 0.90432 | 0.9001 | 1 | 0.95263 | 0.95269 | 0.96344 | 1.0818
 | 1 | 0.83794 | 0.7467 | 0.2545 | 0.34214 | 0.39069 | 0 | 1 | 0.77351 | 0.67393 | 0.49284 | 0.33833 | 0.25234 | 0.038749 | 0 | 0 | 0 | 1 | 0.88598 | 0.56682 | 0.47314 | 0.2433
Chart: A) pH
| 0 | 20 | 50 | 123 | 153 | 261 | 434.3 | 0 | 15 | 20 | 60 | 90 | 220 | 250 | 280 | 290 | 460 | 0 | 66.599999999999994 | 87.5 | 177.1 | 291.7 | 455.9 | 0 | 2 | 26 | 93 | 298
pH | 11.6 | 11.4 | 11.3 | 11.2 | 11.2 | 10.4 | 9.9 | 12.68 | 12.45 | 12.48 | 12.39 | 12.36 | 12.34 | 12.56 | 12.15 | 12.33 | 11.95 | 11.51 | 11.56 | 11.56 | 11.56 | 11.4 | 11.32 | 11.73 | 11.66 | 11.63 | 11.49 | 10.88
Chart: B) Ca
| 0 | 20 | 50 | 123 | 153 | 261 | 434.3 | 0 | 15 | 20 | 60 | 90 | 220 | 250 | 280 | 290 | 460 | 0 | 66.599999999999994 | 87.5 | 177.1 | 291.7 | 455.9 | 0 | 2 | 26 | 93 | 298
C/Co [Ca] | 1 | 0.98403 | 0.95806 | 0.90776 | 0.87236 | 0.85364 | 0.82656 | 1 | 0.94647 | 0.94119 | 0.90834 | 0.88958 | 0.84934 | 0.83251 | 0.80272 | 0.76069 | 0.75594 | 1 | 0.9695 | 0.87831 | 0.86441 | 0.77517 | 0.6832 | 1 | 0.94656 | 0.88688 | 0.89324 | 0.81545
Chart: D) V
| 0 | 20 | 50 | 123 | 153 | 261 | 434.3 | 0 | 15 | 20 | 60 | 90 | 220 | 250 | 280 | 290 | 460 | 0 | 66.599999999999994 | 87.5 | 177.1 | 291.7 | 455.9 | 0 | 2 | 26 | 93 | 298
C/Co [V] | 1 | 0.9555 | 0.89431 | 0.81824 | 0.75954 | 0.67302 | 0.55462 | 1 | 0.92677 | 0.92152 | 0.90217 | 0.8388 | 0.81894 | 0.76642 | 0.74599 | 0.67063 | 0.61559 | 1 | 0.86471 | 0.84155 | 0.71762 | 0.66854 | 0.66746 | 1 | 0.89106 | 0.88363 | 0.89067 | 0.78246
Chart: E) Fe
| 0 | 20 | 50 | 123 | 153 | 261 | 434.3 | 0 | 15 | 20 | 60 | 90 | 220 | 250 | 280 | 290 | 460 | 0 | 66.599999999999994 | 87.5 | 177.1 | 291.7 | 455.9 | 0 | 2 | 26 | 93 | 298
C/Co [Fe] | 0.99993 | 0.89668 | 0.86022 | 0.86349 | 0.83532 | 0.69713 | 0.48365 | 0.99997 | 0.83247 | 0.78867 | 0.661 | 0.57816 | 0.56976 | 0.63883 | 0.49241 | 0.48368 | 0.46125 | 1 | 0.92514 | 0.82575 | 0.79176 | 0.72143
Co = 104 ±31 ppm
Co = 127 ±57 ppm
Co = 58 ±8 ppb
Si Co = 1300 ±340 ppb
Al Co = 129 ±39 ppb
Chart: C) K
| 0 | 20 | 50 | 123 | 153 | 261 | 434.3 | 0 | 15 | 20 | 60 | 90 | 220 | 250 | 280 | 290 | 460 | 0 | 66.599999999999994 | 87.5 | 177.1 | 291.7 | 455.9 | 0 | 2 | 26 | 93 | 298
C/Co [K] | 1 | 1.0551 | 1.06 | 1.0592 | 1.0445 | 0.97577 | 1.0145 | 1 | 0.9928 | 1.0043 | 0.99817 | 0.99567 | 0.99704 | 0.98706 | 0.98644 | 0.92215 | 0.91755 | 1 | 1.0701 | 1.021 | 1.0371 | 0.94072 | 0.93813 | 1 | 0.96293 | 0.94806 | 0.94725 | 0.97509
pH reduction & Ca removal
Concurrent Trace Metal Removal
No change in conservative elements (i.e. no dilution)

## Slide 22: Experimental
Slag Leachate
Site Leachate – Ca(OH)2 type ~35 ppb V (+Fe)
Slag Leachate – Ca2SiO4 type ~ 500 ppb V (+Si)
Sim. Leachate – 10 % Ca(OH)2 + 2500 ppb VO43- (for XAS)
All initially pH ~12 & CO2 free

## Slide 23: Results – pH

## Slide 24: Results – Calcium
Graph of C/Co [Ca] vs pH– three leachates CaCO3 only systems
Site [Ca] = 194 ppm
Slag [Ca] = 89 ppm
Sim. [Ca] = 75 ppm
Total [Ca] removal very similar in all systems; ~60-80 ppm

## Slide 25: Results – Vanadium
Graph of C/Co [V] vs pH– three leachates CaCO3 only systems
Site [V] = 35 ppb
Slag [V] = 510 ppb
Sim. [V] = 2510 ppb
[V] removed: Site = ~13 ppb; Slag = ~30 ppb; Sim. = 400 ppb

## Slide 26: Results – Fe
Site [Fe] = 166 ppb
Slag & Sim. [Fe] = n.d.
Sim. [Si] = n.d.
Site [Si] = 1.6 ppm
Slag [Si] = 21 ppm
Results – Si
60-70 ppb Fe removed in Site leachate system

## Slide 27: TEM – site leachate ppt
SAED
Calcite
Fe-O rich particles
Low res Bright field TEM
Hi res TEM
0.145 nm
0.250 nm
Chart: Energy (keV)
EDS spectra
Fe
Fe
Fe
Si
Ca
Ca
O
Cu
Na
C
P
S
Cl
Al

## Slide 28: Goethite amended systems
Graph of C/Co [V] vs pH– three leachates FeOOH systems
unamended data
Site
Slag
Sim.

## Slide 29: Vanadium K-edge XANES
Chart: Energy (eV)
0.5
V5+ aqueous
V5+-Kaolinite
V5+-Al(OH)3
V5+-FeOOH
Sim. +FeOOH
Slag +FeOOH
Site +FeOOH
Sim. +Kaolinite
Slag +Kaolinite
Site +Kaolinite
Sim. unamend
Slag unamend
Site unamend
Diamond Light Source, UK, Beamline i18
Data collected from CaCO3 precipitates (pH ~8)
All Vanadium present as V5+

## Slide 30: V – XANES interpretation
(Td) V5+
(Py) V5+
(Oh) V3+
(Oh) V5+
(Oh) V4+
(Py) V4+
V5+-Al(OH)3
V5+-FeOOH
NaVO3
Experimental Samples
Measurement uncertainty
V5+-Kaol.
Distortion in VO4 tetrahedral leads to reduced peak intensity
adsorption / incorporation

## Slide 31: V-FeOOH EXAFS
Chart: r (Å)
Peacock and Sherman, 2004
Chart: k (Å-1)
A)
B)
A) Sim. +FeOOH (0.2% w/w)
B) V-FeOOH std. (2% w/w)
VO4
V-Fe

## Slide 32: Part 2 Summary
Groundwater outflow
Steel Slags
CO2 in gassing = modest V removal via sorption to neoformed phases
Interaction with stream sediments = complete V removal via adsorption to iron(oxy)hydroxides
Vanadium will accumulate in near field sediments; no far field impacts

## Slide 34
Chart: [Ca2+] mol L-1
| 0.1 | 0.01 | 1E-3 | 1E-4 | 1.0000000000000001E-5 | 9.9999999999999995E-7
[VO43-] | 3.2734e-08 | 1.0351e-06 | 3.2734e-05 | 0.0010351 | 0.032734 | 1.0351
 | 1.6845e-05
 | 9.6629e-06
 | 0.0005865
 | 1.6845e-05
 | 1.6845e-05
 | 1.6845e-05
 | 0.0005865
 | 1.6845e-05
 | 0.023
 | 2.9676e-07
 | 0.023
Oversaturated
Undersaturated
Calcite / atm. CO2
~4000 ppb V
Ca(OH)2
~15 ppb V
Aerobic expt. 1000-3000 ppb V
Ca2SiO4 / Ca-Si-H
Anaerobic expt.
200-500 ppb V
Site Leachates
20-100 ppb V
Acute Tox.
Chronic Tox.
280 ppb
19 ppb